## Slide 1
Radboud University Nijmegen, the Netherlands
Inge van Rens
1 July 2025
Update on hydrogenated graphene in Nijmegen

## Slide 2: Hydrogenated graphene - progress
Sequential hydrogen exposure
Stability study
Temperature dependence
Quantum Hall effect
Raman spectroscopy
Simulations
Radiation response

## Slide 3: Hydrogenated graphene - progress
Sequential hydrogen exposure
Stability study
Temperature dependence
Quantum Hall effect
Raman spectroscopy
Simulations
Radiation response

## Slide 4: Hydrogen plasma exposure
H inlet
Vacuum pump
Sample location
electrodes

## Slide 5: Hydrogenation process
Start with annealed sample
Exposed 1 mbar hydrogen plasma for 5 minutes
Exposed to air for 10 minutes
Repeat until we reach an interesting state
Result looks similar to earlier samples
Notes: Hydrogenated both samples, meanwhile cooling them with liquid nitrogen to check when the band gap starts to open -> 80s for first sample, 25 min for second

## Slide 6: Raman spectroscopy
D
G
2D
D+D’
Notes: D peak is measure for impurities, appears after hydrogen exposure
Also D’ as shoulder to G

## Slide 7: Relative size of the Raman peaks
Notes: Relative size of D and G peaks is often used to determine level of disorder in graphene, ours is not very high, but cannot be easily compared quantitatively

## Slide 8: Relative size of the Raman peaks
J. Phys. Chem. C 2011, 115, 5, 1422–1427
Notes: Our laser was at 532 nm or 2.33 eV/photon, corresponding to the green triangles. In literature the D/G goes up to 5, but we only see it go to 2 in an outlier

## Slide 9: Simulation method
Scaling the size of the graphene sheet

## Slide 10: Simulation method
Scaling the size of the graphene sheet
Add 1 hydrogen atom

## Slide 11: Simulation method
Scaling the size of the graphene sheet
Add 1 hydrogen atom
Calculate effective band structure
Get effective electron mass from second derivative of the dispersion

## Slide 12: Simulations
Pristine graphene
No band gap
Linear dispersion near K

## Slide 13: Simulations
0.5% hydrogen coverage
Small band gap
Band structure nearly linear near K

## Slide 14: Simulations
1% hydrogen coverage
Small band gap
Strongly curved band structure near K

## Slide 15: Simulations
2% hydrogen coverage
Band gap increases
Curvature decreases

## Slide 16: Simulations
3% coverage

## Slide 17: Simulations summary

## Slide 18: Simulations
12.5% coverage
Insulating material

## Slide 19: Conclusions
We have exposed graphene to a hydrogen plasma
Raman spectroscopy confirms the presence of hydrogen
A band gap starts to open
The Landau level distance becomes linear in B
Simulations show that our hydrogen coverage is around 3-4%

## Slide 20: Ptolemy implications
Hydrogenation impacts resistance
Temperature dependence: will the target be cryogenic?
Can we dope the target to reduce resistance at higher hydrogenation?

## Slide 21
Backup slides

## Slide 22: The Nijmegen Group
Uli Zeitler
(RU HFML-FELIX)
Nicolo de Groot
(RU IMAPP)
Oleksandr Zheliuk
(RU HFML-FELIX)
Nicoleta Cucu-Laurenciu
(RU IMAPP)
Inge van Rens
(RU IMAPP)
Martijn Velders
(RU IMAPP)
Bram Breugelmans
(RU HFML-FELIX)
Thomas Derks
(RU HFML-FELIX)
And our students:

## Slide 23: Simulations – 50% coverage
1 hydrogen per 2 carbon

## Slide 24: Simulations – 100% coverage
2 hydrogen per 2 carbon

## Slide 25: Compare simulations to hydrogenation results

## Slide 26: Graphene Field Effect Transistor
SiO2
gate insulator
Si backgate
Au contacts
graphene
Graphenea, GFET-S10 data sheet
Geim, A. K. & Novoselov, K. S. The rise of graphene. In Nanoscience and technology: a collection of reviews from nature journals, 11–19 (World Scientific, 2010)

## Slide 27: Hydrogenation process
Start with annealed sample
Exposed 1 mbar hydrogen plasma for 5 minutes
Exposed to air for 10 minutes
Repeat until we reach the wanted state
Notes: Hydrogenated both samples, meanwhile cooling them with liquid nitrogen to check when the band gap starts to open -> 80s for first sample, 25 min for second

## Slide 28: Temperature dependence
Peak resistance increased as temperature decreased
Pristine state: no temperature dependence
From vrh fit: band gap 2.1±0.4K

## Slide 29: Temperature dependence
Neutrality point shifted
Temperature dependence similar
From vrh fit: band gap 2.6±1.1K

## Slide 30: Temperature dependence
Compare samples g12 and g3
Similar band gap opening
Band gap is far smaller than for a fully hydrogenated graphene sample (Elias et al., Science 323, 610-613 (2009))

## Slide 31: Magnetic field effects
A. J. M. Giesbers, U. Zeitler, M. I. Katsnelson, L. A. Ponomarenko, T. M. Mohiuddin, and J. C. Maan, Quantum-Hall Activation Gaps in Graphene. In PRL 99, 206803 (2007)
Notes: At nu -2: only localised states -> no charge carriers -> no potential difference? Check with Uli

## Slide 32: Quantum Hall Effect
𝜈=-2
𝜈=+2

## Slide 33: Quantum Hall Effect
𝜈=-2
𝜈=-6

## Slide 34: Activation energy
Notes: Pristine graphene: activation sqrt in B
Hydrogenated becomes linear due to curved band structure

## Slide 35: Activation energy
Activation gap depends on Landau level broadening and peak-to-peak distance
Effective electron mass can be extracted from the slope of the activation gap
25 minutes of plasma exposure, filling factor -2:
30 minutes of plasma exposure, filling factor -2:
For pristine graphene, Δ∝

## Slide 36: Simulations
Pristine graphene
12.5% H coverage

## Slide 37: Simulations
Pristine graphene
25% H coverage